| Hardness | Mineral | Associations and Uses |
| --- | --- | --- |
| 1 | Talc | Talcum powder. This is a finely ground magnesium silicate based rock. |
| 2 | Gypsum | Plaster of Paris. Gypsum is formed when seawater evaporates from the Earth’s surface. |
| 3 | Calcite | Limestone and many sea shells contain calcite. |
| 4 | Fluorite | Fluorine in fluorite is used to hep protect teeth against decay. |
| 5 | Apatite | A mineral found in the enamel of the teeth of animals |
| 6 | Orthoclase | Orthoclase is a feldspar, and in German, "feld" means "field". Feldspar is the most common mineral in the Earth’s rocks |
| 7 | Quartz | A mineral found in granite, sandstones and many other rocks. Since it is so hard, although the rocks containing it are broken down, it finds its way, as tiny resistant grains into sand and then into other rocks. |
| 8 | Topaz | Emerald and aquamarine are both varieties of beryl with a hardness of 8. |
| 9 | Corundum | Sapphire and ruby are varieties of corundum. Twice as hard as topaz. |
| 10 | Diamond | Used in jewellery and cutting tools. Diamond is about four times as hard as corundum. |

Hardness of some other easily found items:

| 2.5 | Fingernail |
| --- | --- |
| 2.5–3 | Gold, Silver |
| 3 | Copper penny |
| 4-4.5 | Platinum |
| 4-5 | Iron |
| 5.5 | Knife blade Human tooth enamel |
| 6-7 | Glass |
| 6.5 | Iron pyrite |
| 7+ | Hardened steel file |

# Text boxes

Moh’s Scale of Hardness   (Frederich Mohs (1773-1839)   Devised in 1812

www.design-technology.info